FLOOR MAT SPECIFICATIONS

1.0 General Specifications

1.1 Scope and Purpose

This document outlines the requirements and specifications needed for an acceptable product for Floor Matting.

1.2 System Description

Floor  mat designed for Heavy Commercial traffic.

Product must comply with all specifications outlined in section 2.0 and 3.0 of this document.

1.3 Warranty

The Floor Mat must be warranted for 4 years against loss of pile fiber.   During the warranty period not more that 15% of pile fibers may be lost due to normal usage and wear.

1.4 Delivery
Deliver Floor Mat to jobsite in new, clean, unopened, original factory packaging of sufficient size and strength to protect materials during transit.
2.0 Product Specifications

2.1 Carpet

Carpet pile must be 100% cut pile nylon.    The fibers must be twisted and Heat set for durability.

2.2 Matting Edge

All Mat edging must be constructed of 100% PVC with no fillers added.   Edging must comply with all safety requirements as outlined in section 3.0 of this document.

All corners must be mitered and reinforced against possible separation failure.

2.3 Backing

The Mat backing must be a multi layered dimensionally stable 100% vinyl backing.   The backing must treated for Anti-Microbial formation.


Backing must secure the product to the floor to meet safety requirements 3.1 as outlined in this document.

2.4 Logo Requirements

Logos must be die/laser cut and securely fastened to the field carpet of the matting system.   Nylon carpet must be used for the logo and comply with section 2.1 of this document.

3.0 Safety

3.1 Government and Regulatory Requirements

Product must comply with the “Americans for Disabilities” act and International Standards.   All aspects of “4.5 Ground and Floor Surfaces” of this act must be complied with.

3.2 Product Safety Specifications

The Floor Mat must pass the following industry recognized flammability tests:

· Flammability
 (0.45 (Class 1) : Radiant Panel ASTM-E-648

· Smoke Density   (450 : NFPA-258-T or ASTM-E-662

· Methenamine Pill Test : Self-Extinguishing  : CPSC-FF-1-70    or  ASTM D 2859

________________________________________________________________________


01/06/2006
Page 2 of 2

