	SYSTEM


	T E C H N I C A L


[image: image1.jpg]CYRUS

SYSTEMS
A Higher Standard






Face Fiber

Construction
Tufted, Cut pile

Face Fiber
100% Nylon, Twisted and Heat Set 

Finished Face Weight
27 oz/sq.yd. (915.5 g./sq.m.)

[image: image2.wmf]Face Fiber  

Cyrus SAFETY Edge

 (A.D.A. Compliant)

100% Nylon Cut Pile

Non-Slip Stronghold

Non-Slip Stronghold Membrane

Multi-Layer Back

Heat Welded

Edge

Gauge
5/32 in. (25.2/10cm)

Finished Pile Height
0.237in. (6.0mm) Avg.

Flammability
(0.45 (Class 1)   :Radiant Panel ASTM-E-648

Smoke Density
(450   :NFPA-258-T or ASTM-E-662

Methenamine Pill Test
Self-Extinguishing   :CPSC-FF-1-70 or ASTM D 2859

Light fastness (AATCC 16E)
(4.0 @ 80 Hrs.

Backing

Primary Precoat
100% Vinyl Non-Aqueous Closed Cell Polymer

Secondary Backing
Reinforced Vinyl Composite Closed Cell Polymer

(Anti-Microbial Treatment)

Structure
Dimensionally Stable Fiberglass Reinforcement

Stronghold(
Type 
Reinforced Composite Backing impregnated

with a chemically inert patented blend.   

System Movement
No movement once installed (no glues / adhesives used)


Reducer

Reducer Type
Extruded unfilled PVC

Incline Ratio
3.75 : 1

Corner Type
Mitered 

Corner Structure
Heat welded and braced with impregnated 

woven polyester fabric


System 

Recommended Traffic
Heavy Commercial

Recommended Maintenance
Extraction

Safety
Complies with the “Americans for Disabilities” 

Act and international standards

System Weight
1.3 Ibs./sq.ft.






800-661-3387









www.cyrussystems.com 




ENTRYWAY





AREA





DIRECTIONAL





ROLL OUT





TECHNICAL











